MARMORINO RESIN

DESCRIPTION

Marmorino Resin 2 parts is a special finish to create flat monolithic decorative surfaces for a particular seamless result.

Made of 2 parts components, high hydraulic resistance binders, selected and examined inert, particular polymers and special additives. (CEMENT FREE).

Marmorino resin has an excellent filling power and It’s also extremely versatile and has an elegant, pleasant and functional aspect, suitable over underfloor heating.(on top of screed)

Marmorino Resin 2 parts is suitable as a decorative covering with a low thickness  (appr. 2/3 mm) , for flooring and walls, offices, exhibition areas, dwellings, bathrooms, stairs, splashback and on every surface where a very valued finish is required.

It is a product that can be compared to natural wood floors, therefore is intended for use in private areas that will not be subjected to heavy use. It is not recommended for use in public areas or places where there is a lot of foot trafic.

COLOURS RANGE

Marmorino Resin 2 parts is sold in white base.

Check our color range on www.venetianplastershop.com.au

Note: Advanced Spirito Libero recomends that our entire range of lime based natural materials is used only by highly skilled or licensed trades people with extensive experience in this field. It is the responsability of the applicator to understand the application method and the procedure involved in order to obtain a satisfactory outcome. Advanced Spirito Libero recomends that architects, builders and clients appoint only experienced applicators in the relevant lime-based materials to ensure they'll be able to deliver the same finish as per the sample shown.

We cannot guarantee that the existing substrate will not move causing our product to delaminate and crack. This is a substrate failure and the movement is beyond our control.   Concrete is variable by nature, cement source, age and quality as well as placement, curing and finishing methods. All this will have an impact on the final appearance/quality of the concrete substrate you will be applying over. Advanced Spirito Libero will not be held responsible for these naturally occurring variations in the finished floor. This Includes subfloor or substrate cracking.

Ensure that a sufficient quantity of the same batch is available to complete the entire job or at least to complete whole sections that will not reveal differences in shade.

Following the Australian Building Code we do not suggest the installation of this product inside the shower area.

Preparation For Wall Application:

| TYPE OF SURFACE | PRELIMINARY TREATMENTS |
| --- | --- |
| Any Surface (except render) | Apply 1 coat of Undercoat Sealer before priming |
| Old plasterworks | Brushing, eventual power washing and a coat of CONSOLIDATING PRIMER. |
| Render/ Base coat render | Coat of PRIMUS NATURALE primer. |
| Medium density | Coat of PRIMUS NATURALE primer. |
| Plasterboard | Coat of PRIMUS NATURALE primer. |
| Plaster | Coat of PRIMUS NATURALE primer. |
| Concrete | Coat of PRIMUS NATURALE primer. |
| Polished lime finishing | Accurate sanding and a coat of PRIMUS NATURALE primer. |
| Washable paints | Coat of PRIMUS NATURALE primer. |
| Non-mineral decorative finishings | Coat of PRIMUS NATURALE primer. |
| Plastic coating | A coat of oil based primer then a coat of PRIMUS NATURALE primer. |

Preparation For Floor:

You must apply one coat of PRIMUS AGGRAPANTE over concrete and existing tiles after sending back ,and then apply one coat of BUILD UP BASE (refer Technical Data Sheet) in conjunction with fiber mesh and let dry for 24 hours .

HOW TO BLEND THE PRODUCT

Marmorino Resin 2 parts is a two part product.

Mix the powder BASE A with the liquid element BASE B, in ratio of 100 parts of “A” and 45 parts of “B”, equivalent to the  45 % of B, as weight.

Remove from the vase the A base sack, pour the B base on the bucket, add in the desired colorant, add the A Base and mix accurately the whole product for approximately  3/5 minutes, till obtain the complete mixture homogenization.

APPLICATION :

FIRST COAT

Product:           Marmorino Resin 2 parts

Apply with a venetian plaster trowel in an equally and uniform way.

Once the first coat is applied, the process has to be complete within 48h.

SECOND COAT

Product:           Marmorino Resin 2 parts

Apply with a venetian plaster trowel evenly in criss cross way.

Proceed when the first coat is completely dry (after min 6/8 hours at 20° C), press and smooth accurately to make a flat surface without irregularities.

THIRD COAT

Product:           Marmorino Resin 2 parts

Apply with a venetian plaster trowel Wet on wet: to complete when the second coat is not perfectly dry yet, but sufficiently hardened (approximately between 2/3 hours at 20° C.), so that the pressure of the venetian plaster trowel lets penetrate the inert on the previous coat.

SURFACE FINISHING

Marmorino Resin 2 parts, for its versatility and ease-application, is perfect for different kind of finishing, depends on the applicator’s ability.

-Contrasted finish: for this type of finishing, use the venetian plaster trowel and rub the surface while the third coat is drying with a hard pressure till get the polishing of the surface. The procedure gets a smooth and pleasant looking with evident contrast draws.

-Velvety finish: for this type of finishing use a stiff plastic trowel, rubbing the surface during the dry phase ( only how is specified on the wet on wet procedure), with the right pressure till get the smoothing. You get a smooth look with chromatic and uniform tones, little contrasted but “velvety”.

-Rustic finish: it can be obtained sanding the surface with an abrasive paper 120/150 grit, highlighting the draw made during the layer and getting an opaque matt surface “rustic”.

PROTECTIVE FINISHINGS

Marmorino Resin 2 parts, for its mineral nature, is a porous and permeable material and requires an adequate surface protection to preserve its beauty and to get a very low maintenance finish.

Apply 2 coats of MARMORINO RESIN SEALER (Refer Marmorino Resin Sealer Technical Data Sheet)

ENVIRONMENTAL CONDICTIONS FOR THE APPLICATION

The ambient temperature must be between a minimum of  +8°C and a maximum of  +30°C. The humidity must be below 85% also in the 24 hours after the application. For the outdoor applications, avoid the windy days. It’s discouraged to apply the product under the sun or the rain.

PRESERVATION

The product keeps unaltered its features for a  period of 12 months if conveniently preserved. Keep away from humidity.

SAFETY REGULATIONS

Avoid the contact with the skin and eyes, if happens, wash abundantly with water. For further information consult  the safety file.

DISPOSAL

The product must be disposed according to the current regulation. Empty buckets must be disposed.

TECHNICAL DETAILS

Aspect

White dust  BASE A – Milky liquid  BASE B

Packaging

Plastic bucket from 13.4   Kg. net weight

Tools for the application

Venetian Plaster Trowel

Specific weight

1,05 ± 0,05 Kg/l  BASE  A

1,00 ± 0,05 Kg/l  BASE  B

Theoretical performance

1,75 ÷ 2,00 Kg/m2 3 coats total

Coarse-grained curve

0,02 ÷ 0,70 mm.

Thickness covering

1,50 ÷ 2,00 mm. 3 coats included

Dry touch

2 hours    with a temperature of  20°C

Dry in depth

24 hours     with a temperature of  a 20°C

Constant Aging

180 days

Upper application

6 hours    with a temperature of  20°C

PH after 30 days

12,5 ± 0,2

Flammability

not flammable  - A1 class