## Slide 1: Development of Test Setup to Support Acoustic Structural Health Monitoring Technique
Erek Croteau
Alex De Sena
Nelson Lezama
Jordan Parris

## Slide 2: Table of Contents
Project purpose and overview
Design schedule and procedures
Analysis of Design
Results, conclusions, and recommendations

## Slide 3: Project Purpose & Overview
Design a hollow model wing section made of a glass fiber composite to use as a test specimen for an acoustic structural health monitoring (SHM) test procedure
Develop a support fixture for use in a wind tunnel
With a developed test system and procedure for acoustic SHM, a quick and inexpensive process can be implemented for different structures
Qantas A380 Wing Damage

## Slide 4: Design Procedures
Design and fabricate a mold (mandrel) to use for creating composite wing sections [February 8 - April 11]
Make composite wing sections with glass fiber composite (Twintex) using the mandrel [April 12 - April 19]
Design and assemble a test set-up for acoustic SHM using the composite wing section [February 22 – April 27]

## Slide 5: Gantt Chart

## Slide 6: Gantt Chart

## Slide 7: Design Procedures – Airfoil Selection
Airfoil must:
  Be symmetric
  Allow 2.5” – 3” of space for microphone and speaker
  Have a minimum resulting chord length
Three different airfoil designs selected
NACA-0018 ultimately selected
  Minimum chord length to achieve 3” mic clearance
  Used in full scale wings
Name | Maximum Height as a Percent of Length | Chord Length to achieve 3” Microphone Clearance (in) | Symmetric
E169 | 14.4% | 20.8 | Yes
Eppler 297 | 11.4 % | 26.3 | Yes
NACA0018 | 18 % | 16.67 | Yes

## Slide 8: Design Procedures – Mandrel Design
Initial design: 23” span, 2.81” max height, 16” chord length, 0.465” wall thickness
Several fabrication processes considered
  3D printing (At UML or AFS)
  Acrylic sheets with foam fill
  Machined aluminum
Design for 3D printing:

## Slide 9: Design Procedures – FEA of Mandrel
1st Test – ABS (Uncapped)
14.7 psi Pressure
Fixed BC on Bottom Face
Max Principal Stress
Displacement
Case | Variable | Value
Mandrel (ABS) | Thickness (in) | 0.425
 | Applied Pressure (psi) | 14.7
 | Max Stress (psi) | 5165
 | UTS (psi) | 5802
 | Max Displacement (in) | 1.02 x 10-4
 | Thickness (in) | 0.500
 | Applied Pressure (psi) | 14.7
 | Max Stress (psi) | 3754
 | UTS (psi) | 5802
 | Max Displacement (in) | 6.576 x 10-5

## Slide 10: Design Procedures – FEA of Mandrel
2nd Test – ABS & ULTEM (Capped); 14.7 psi Pressure
Max Principal Stress
Displacement
Case | Variable | Value
Mandrel (ABS) | Thickness (in) | 0.465
 | Applied Pressure (psi) | 14.7
 | Max Stress (psi) | 1030
 | UTS (psi) | 5802
 | Max Displacement (in) | 0.0286
Mandrel (ULTEM) | Thickness (in) | 0.465
 | Applied Pressure (psi) | 14.7
 | Max Stress (psi) | 1024
 | UTS (psi) | 17000
 | Max Displacement (in) | 0.0133
Rod | Applied Moment (lb-in) | 84 (5.25 lb. weight)
 | Max Stress (psi) | 855.6
 | UTS (psi) | 40000
 | Max Displacement (in) | 3.08 x 10-3

## Slide 11: Design Procedures –Mandrel Material and Cost Considerations and Re-design
Glass transition temperature must be reasonably higher than cure temperature of 160°C
  ULTEM 1010– Glass transition temperature of 215°C
For one canister of ULTEM 1010 – roughly volume – leads to a maximum of 6.5 inch span

## Slide 12: Design Procedures –Mandrel Fabrication
6.5 inch-span mandrel designed and created with a sparse fill

## Slide 13: Design Procedures – Composite Fabrication
Composite model was produced using Twintex
  Thermoplastic resin makes it ready-to-use and reduces preparation time
  Fast processing cycle time under high temperatures and relatively low pressures
  Recommended for vacuum-molding processes

## Slide 14: Design Procedures – Composite Fabrication
Four layers of Twintex sheets cut to strands at…
90-degrees
45-degrees
45-degrees
90-degrees

## Slide 15: Design Procedures – Composite Fabrication
Mandrel with Layers of Twintex

## Slide 16: Design Procedures – Composite Fabrication
Additional vacuum-bagging materials
  Release peel ply
  Breather or bleeder
  Vacuum-bagging film

## Slide 17: Design Procedures – Composite Fabrication
Mandrel with Layer of Release Peel Ply

## Slide 18: Design Procedures – Composite Fabrication
Mandrel with Addition of Layer of Breather

## Slide 19: Design Procedures – Composite Fabrication
Mandrel with Addition of Layer of Vacuum-Bagging Film

## Slide 20: Design Procedures – Composite Fabrication
Mandrel coated with PARTALL Paste #2
  General purpose polishing compound
  Designed for thermoset molding resins

## Slide 21: Design Procedures – Composite Fabrication
Twintex layers tightly wrapped around mandrel
Heat gun and clamps used to begin fusing process at trailing edge with addition of each Twintex layer
Kapton tape wrapped around span of mandrel (by trailing edge) to ensure fusion

## Slide 22: Design Procedures – Composite Fabrication
Wrapped Twintex layers and mandrel centered and placed on vacuum-bagging materials
Ply and breather neatly folded over Twintex layers
    Leading edge of Twintex layers and mandrel aligned with and touched fold of vacuum-bagging materials

## Slide 23: Design Procedures – Composite Fabrication
Failure to align leading edge and fold resulted in deformation by leading edge

## Slide 24: Design Procedures – Composite Fabrication
Base of vacuum connector placed on breather by trailing edge of Twintex layers
Vacuum tape placed precisely along exposed edges of vacuum-bagging film
Film neatly folded over and pressed along vacuum tape
Small hole introduced and body of vacuum connector screwed onto vacuum bag

## Slide 25: Design Procedures – Composite Fabrication
Mandrel with Layers of Twintex inside Vacuum Bag

## Slide 26: Design Procedures – Composite Fabrication
Vacuum bag held up by end closest to trailing edge and vacuum tube connected to vacuum connector
Pressure valve turned and vacuum bag began to experience vacuum pressure (pressure of about 18 inHg)
After examining bag, vacuum tube disconnected and reconnected within VWR 1600 HAFO Series (Model 1685) oven set to 160°C

## Slide 27: Design Procedures – Composite Fabrication
Vacuum Bag in Oven

## Slide 28: Design Procedures – Composite Fabrication
Initially, much smaller oven was used
Excess vacuum-bagging film touching walls of oven reached temperatures significantly higher than 160°C
  Film melted and burned because it exceeded temperature threshold

## Slide 29: Design Procedures - Composite Fabrication
Vacuum bag left in vacuum in oven for period of one hour
After curing, oven turned off and bag left in vacuum in oven to cool for 30 minutes
After cooling, composite model and mandrel removed from bag

## Slide 30: Design Procedures – Composite Fabrication
Cured Composite Model and Mandrel

## Slide 31: Design Procedures – Wing Support Design
Wind tunnel test area: 3’ x 4’ x 25”
Support links available
For 2-dimensional flow representation, vertical wing orientation is preferred
Wing section must be completely sealed

## Slide 32: Design Procedures – Wing Support Design
Caps used to seal wing section
Rods press-fit into caps to support the wing section
Shaft collars purchased from McMaster-Carr
Manufacturing setbacks
  Wind tunnel maintenance – new top plate cannot be created
  Unavailability of CNC machines – caps hand-cut with wood

## Slide 33: Design Procedures – Intended Final Support System Design

## Slide 34: Final Test Set-Up
Frame Made of 80/20 Extrusions

## Slide 35: Final Test Set-Up
Support rods cut/lathed
Rods press-fit into caps

## Slide 36: Final Test Set-Up
Composite Section Mounted on Final Test Set-Up Secured by Clamps

## Slide 37: Analysis of Design
Degrees of freedom are fixed
About 3 inches of space allowed for microphone and speaker
Composite section is capable of being sealed and unsealed (maintaining accessibility)

## Slide 38: Results and Conclusions
The final assembly is practical and suitable for SHM testing
Test setup is sturdy and easy to work with inside the wind tunnel
The fixture allows the angle of attack to be changed if necessary
Composite wing can be sealed to form an isolated chamber with enough room for the mounting of equipment
ULTEM 1010 proved to be the correct choice for this type of curing procedure
Twintex did not cure as well as expected so some gaps may still be present between the fibers

## Slide 39: Recommendations
Adhering egg crate foam to the inside of the caps to isolate the acoustics of the caps from the wing chamber
Base line measurements should be taken at fixed wind speeds before damages are introduced to the composite wing
If Twintex does not provide a completely sealed chamber, an alternate material with a more reliable curing process should be considered

## Slide 40
Thank You!
Questions?